# Text boxes

Polyurethane, hardness 75 SH (medium), minimum slope with good sharpening.

UVILABEL

UVILABEL inks can be mixed with the LABELMAT range to adjust brilliance.

Although the products selected for the formulation are not dangerous as such, contact can cause allergic reactions in some particularly sensitive individuals. Ink soils on the skin should be cleaned as soon as possible with soapy water. In any case, refer directly to the safety sheets.

After extraction of the ink, open pots need to be carefully and promptly closed. Artificial or natural light can cause the start of polymerization and lead to the formation of a thin skin at the surface. For this reason, it is advisable to work in a low lighting or safelight environment.

One year in its original packaging stored in between + 5°C and + 35°C.

The UVILABEL ink will polymerize under a UV dose in the range of   60 to 100 MJ/cm², depending on the mesh and color used.

It is possible to speed up the drying process by adding 3 to 5% of LA202. Adding the LA202 will also boost the glossiness.

UVILABEL 1 kg

UVILABEL 5 kg

Cleaning with the solvent 77BIO, 77NETX2 or X3 is recommended.

UVILABEL inks are ready to use but can be diluted by a few percent using the UV201 thinner.

Fabrics: all mesh types from 100 to 165 threads/cm.

Reports: emulsions and films must be solvent resistant.

- Aspect

Glossy on non-absorbent substrates.

- Applications

Printing on paper labels, polyethylene and top coated polypropylene.

- Major advantages

Flexible and resistant, fast drying, outstanding stability inside screen. Suitable for hot foil printing and embossing.

Juice resistant.

- Printing

- Roll and flat roll machines for continuous label printing.

19/01/2016

Racle polyuréthane souple, 65 Shore afin d’obtenir un maximum de dépôt

UV RELEX  1kg

UV RELEX 5 kg

L’encre UVRELEX est prête à l’emploi.

Nous préconisons le solvant de nettoyage 77NETX2 ou X3